COMPOSITION OF CANADIAN COINS

The following information, available from the Canadian Mint, is invaluable for teachers wishing to make up a lab involving the analysis of currency. Thank you to Gordon Gore for referring me to this web site.
Reference: http://www.mint.ca/en/collectors_corner/circulation

# Value Years Mass (g) Composition
____	______	_______	____________________________

1¢	1908-20	5.67	95.5% Cu, 3.0% Sn, 1.5% Zn
1920-41	3.24	95.5% Cu, 3.0% Sn, 1.5% Zn
1942-77	3.24	98.0% Cu, 0.5% Sn, 1.5% Zn
       1978-79	3.24	98.0% Cu, 1.75% Sn, 0.25% Zn
1980-81	2.8	98.0% Cu, 1.75% Sn, 0.25% Zn
1982-96	2.5	98.0% Cu, 1.75% Sn, 0.25% Zn
       1997-99	2.25	98.4% Zn, 1.6% Cu plating
2000-	2.35	94.0% steel, 4.5% Cu, 1.5% Ni, (*) (NOTE: Magnetic!)

(*)	Note that some pennies in 2000-01 had copper-plated steel compositions, as evidenced by a small “P” under the Queen.

  5¢	1908-19	1.167	7.5% Cu, 92.5% Ag
1920-21	1.167	20% Cu, 80% Ag
1922-42	4.54	99% Ni
1942-43	4.54	88% Cu, 12% Zn
1944-45	4.54	chrome plated steel
1946-51	4.54	99.9% Ni
1951-54	4.54	chrome plated steel
1955-81	4.54	99.9% Ni
1982-99	4.6	75% Cu, 25% Ni
2000-	3.95	94.5% steel, 3.5% Cu, 2% Ni plating

 10¢	1908-10	2.32	7.5% Cu, 92.5% Ag
1910-11	2.33	7.5% Cu, 92.5% Ag
1920-67	2.33	80.0% Ag; 20.0% Cu
1968-77	2.07	99.9% Ni
1978-99	2.07	99% Ni
2000-	1.75	92% steel, 5.5% Cu, 2.5% Ni plating

 25¢	1908-10	5.81	7.5% Cu, 92.5% Ag
1910-19	5.93	7.5% Cu, 92.5% Ag
1920-67	5.83	80.0% Ag; 7.5% Cu
       1967-68	5.05	50.0% Ag; 50.0% Cu
       1968-99	5.05	99.9% Ni
       2000-	4.4	94% steel, 3.8% Cu, 2.2% Ni plating

 $1	1987-	7	91.5% Ni electroplated with 8.5% bronze plating

$2	1996-	7.3	outer ring = 99% Ni
Inner core = 92% Cu, 2% Ni, 6% Al