STRUCTURE DETERMINATION OF  2 - HYDROXY ETHYL METHACRYLATE  COPOLYMERS WITH METHYL ACRYLATE & STYRENE  BY NMR SPECTROSCOPY  by Dr. Sunita Hooda
STRUCTURE DETERMINATION OF
2 - HYDROXY ETHYL METHACRYLATE COPOLYMERS WITH METHYL ACRYLATE & STYRENE BY NMR SPECTROSCOPY
by
Dr. Sunita Hooda
DEPARTMENT OF CHEMISTRY
ACHARYA NARENDRA DEV COLLEGE
GOVINDPURI, KALKAJI
DELHI UNIVERSITY
NEW DELHI – 110 019

---
Approved Objectives of the Proposal
Study 1H NMR and 13C NMR spectra of homo and copolymers for the characterization of copolymers.
Determine conformation of polymer chain using 2D-NMR Data (HSQC, COSY and TOCSY)
Prepare copolymers of 2-HEMA with methyl acrylate, methyl methacrylate, styrene, N–Vinyl Pyrrolidone, 2- Vinyl Pyridine, Vinyl acetate, Methacrylonitrile and Vinylidene chloride monomers by various methods of polymerization.
Prepare poly (2-hydroxy ethyl methacrylate) by various methods of polymerization .
Obtain information about intra-molecular (sequence distribution and tacticity) and intermolecular (chemical composition and molar mass distribution) structure.
The term microstructure is used to describe the specific repeat unit structure, sequencing of the repeat units, average composition, co-monomer distribution and number-average sequence length of monomer addition.
Investigate microstructure of biomedically important 2-HEMA copolymers and develop structure property relations

---
Applications of HEMA
Applications of HEMA
Exhibit hydrophilic and hydrophobic properties by copolymerization with other acrylates.
Used as hydrogels and biocompatible materials with excellent tolerance and good stability.
Preferred basic material for the construction of soft contact lenses, surgery and clinical medicine and drug delivery system.
  Applications of NMR
Physical and chemical properties of polymers are fundamentally influenced by the microstructure.
NMR is probably the best tool to determine the microstructure of polymers as the chemical shifts are sensitive to configurational as well as compositional sequences.

---
Methodology
Preparation of copolymers: Various polymers and copolymers of 2-HEMA with methyl acrylate, methyl methacrylate,styrene, N- Vinyl Pyrrolidone, 2-vinyl pyridine, methacrylonitrile and vinylidene chloride were prepared by different methods of polymerization. The copolymers of different composition were prepared by varying the feed in composition in all copolymer series.
Composition Determination: Composition of various copolymers were determined using elemental (C, H & N) analyses, 1H and 13C NMR spectra of copolymers.
Reactivity Ratios Determination: The composition of various copolymers were utilized to determine reactivity ratios of monomers in copolymers using a non-linear least square error-in-variables method (EVM) and linear methods e.g. Kelen-Tudos.
GPC Measurement: Molecular weight of the copolymers were determined form GPC technique, which in turn were used to study the effect of molecular weight distribution on the properties of copolymers

---
Experimental
Experimental
Purification of Monomers
Preparation of Homopolymers
Preparation of Copolymers
NMR Analysis
1D NMR
1H, 13C{1H}, DEPT- 90, DEPT-135
2D NMR
Heteronuclear Single Quantum Coherence (HSQC), Total Correlation Spectroscopy (TOCSY), Heteronuclear Multiple Bond Correlation (HMBC)

---
Composition Determination of HEMA/MA Copolymers
Composition Determination of HEMA/MA Copolymers
Copolymer composition data of H/M copolymers
The 1H NMR spectrum of H/M copolymer (FH = 0.53) in CD3OD.
0.81
0.55
HM5
5.
0.64
0.33
HM4
4.
0.53
0.23
HM3
3.
0.46
0.18
HM2
2.
0.35
0.12
HM1
1.
FH
f­H
Sample No.
S.No.

---
Reactivity Ratios Determination of HEMA/MA Copolymers
Reactivity Ratios Determination of HEMA/MA Copolymers
Kelen-Tudos (KT) method
rH = 3.31  0.08
rM = 0.23  0.00
Error in Variable Method (EVM)
rH = 3.32
rM = 0.23

---
13C {1H} NMR Studies
13C {1H} NMR Studies
  The DEPT-135 NMR spectrum of H/M
  copolymer (FH = 0.53) in CD3OD.
The 13C1H} NMR spectrum of H/M copolymer (FH = 0.53) in CD3OD

---
The expanded carbonyl carbon regions of H/M copolymers with compositions (FH =):a) 1.00 b) 0.81, c) 0.53, d) 0.35 and e) PMA
The expanded carbonyl carbon regions of H/M copolymers with compositions (FH =):a) 1.00 b) 0.81, c) 0.53, d) 0.35 and e) PMA
  Assignment of carbonyl carbon
  resonances of H/M copolymers
  from13C{1H} NMR spectra.
MMM
176.70
6.
MMH
177.30
5.
MMH + HMH
177.82
4.
MHM
178.28
3.
HmHrH + HHM
178.72
2.
HrHrH
179.75
1.
Assignment
Peak Position
(13C{1H}NMR; ppm)
S. No.

---
The expanded DEPT-90 spectra of a) PMA and H/M
copolymers with compositions (FH =): b) 0.35, c) 0.53
And d) 0.81 in CD3OD at 25°C

---
The expanded -methyl region in 13C1H} NMR spectrum of a) HEMA and H/M copolymers with compositions (FH =): b) 0.81, c) 0.53 and d) 0.35 in CD3OD.
The expanded -methyl carbon regions of 2D HSQC spectra of H/M copolymers with compositions (FH =): a) 0.35, b) 0.53 and c) 0.81
23.20 / 1.30
23.15
HmHmM
7.
22.53 / 1.45
22.50
HmHmH
6.
21.55 / 1.38
21.50
MrHrM
5.
21.05 / 1.28
21.05
HrHmM
4.
19.82 / 1.31
19.80
HrHmH
3.
18.80 / 1.20
18.80
HrHrM
2.
17.76 / 1.15
17.75
HrHrH
1.
Peak Position
(2D HSQC; 13C/1H; ppm)
Peak Position
(13C{1H}NMR; ppm)
Peak Assignments
Peak No.

---
Structure of HH, HM and MM diads.
Structure of HH, HM and MM diads.

---
The expanded -methylene carbon regions of 2D HSQC spectra of H/M copolymers with composition (FH =): a) 0.35, b) 0.53 and c) 0.81
The expanded -methylene carbon regions of 2D HSQC spectra of H/M copolymers with composition (FH =): a) 0.35, b) 0.53 and c) 0.81
36.05/1.76
MMmMM(Hb)
30.
36.05/1.91
MMrMM
29.
36.05/2.07
MMmMM(Ha)
28.
37.80/1.65
HMmMM(Hb)
27.
37.80/1.85
HMrMM
26.
37.80/2.03
HMmMM(Ha)
25.
39.18/1.65
HMmMH(Hb)
24.
39.80/1.88
HMrMH
23.
39.18/2.04
HMmMH(Ha)
22.
43.45/1.64
MHmMM(Hb)
21.
43.45/1.90
MHrMM(Hb)
20.
43.45/2.05
MHrMM(Ha)
19.
43.45/2.32
MHmMM(Ha)
18
45.65/1.63
MHmMH/HHmMM(Hb)
17.
45.65/1.92
MHrMH/HHrMM(H)
16.
45.65/2.05
MHrMH/HHrMM(Ha)
15.
45.65/2.32
MHmMH/HHmMM (Ha)
14.
48.30/1.63
HHmMH(Hb)
13.
48.30/1.87
HHrMH(Hb)
12.
48.30/2.06
HHrMH(Ha)
11.
48.30/2.27
HHmMH(Ha)
10.
51.74/2.00
MHmHM(Hb)
9.
51.74/2.13
MHrHM
8.
51.74/2.35
MHmHM(Ha)
7.
53.18/1.93
MHmHH(Hb)
6.
53.18/2.05
MHrHH
5.
53.18/2.31
MHmHH(Ha)
4.
55.25/1.86
HHmHH(Hb)
3.
55.25/2.25
HHrHH
2.
55.25/2.37
HHmHH(Ha)
1.
Peak Position (2D HSQC; 13C/1H; ppm)
Cross-Peak Assignment
Cross Peak No.

---
1H-1H cross correlation between non equivalent geminal protons of H/M -copolymers observed from 2D TOCSY
1H-1H cross correlation between non equivalent geminal protons of H/M -copolymers observed from 2D TOCSY
The 2D TOCSY spectrum of H/M copolymers with composition (FH =):a) 0.35, b) 0.53 and c) 0.81
2.55 /2.33
CH2 of MmH (Ha)
CH of M
10’
2.55 /2.05
CH2 of MrH(Ha) /
MmM(Ha)
CH of M
9’
2.55 /1.68
CH2 of MmH (Hb)
CH of M
8’
2.06 /1.78
CH2 of MMmMM (Hb)
CH2 of MMmMM (Ha)
7’
2.04 /1.65
CH2 of HMmMM(Hb)
and HMmMH (Hb)
CH2­ of HMmMM (Ha)
and HMmMH (Ha)
6’
2.05 /1.90
CH2 of HrM (Hb)
CH2 of HrM (Ha)
5’
2.30 /1.65
CH2 of HmM (Hb)
CH2 of HmM (Ha)
4’
2.35 /2.00
CH2 of MHmHM (Hb)
CH2 of MHmHM (Ha)
3’
2.33 /1.93
CH2 of MHmHH (Hb)
CH2 of MHmHH (Ha)
2’
2.32 /1.85
CH2 of MrH(Hb) / MrM
CH2 of HHmHH (Hb)
CH of M
CH2 of HHmHH (Ha)
1’
Proton II
Proton I
Peak Position (2D TOCSY; 1H / 1H; ppm)
Coupled Protons
Correlation Peak No.

---
Coupling of carbonyl carbon with methyl, methine and methylene protons of H/M copolymers based on 2D HMBC spectra
Coupling of carbonyl carbon with methyl, methine and methylene protons of H/M copolymers based on 2D HMBC spectra
The 2D HMBC spectra of H/M copolymers showing coupling of carbonyl carbon with methyl, methine and methylene protons of compositions (FH =): a) 0.35, b) 0.53 and c) 0.81
CH of MMM
CO of MMM
176.70 / 2.54
17.
CH2 of HmM (Ha)
CO of MMH
177.30 / 2.34
16.
CH2 of HrM (Ha)
CO of MHM
178.35 / 2.25
15.
CH2 of MmM (Ha)
CO of MMH
177.30 / 2.10
14.
CH2 of MmM (Ha)
CO of MMM
176.69 / 2.09
13.
CH2 of HrM(Hb)
CO of MMH + HMH
177.85 / 1.87
12.
CH2 of MMrMM
CO of MMM
176.70 / 1.93
11.
CH2 of MmM (Hb)
CO of MMM
176.60 / 1.71
10.
CH2 of MmM (Hb)
CO of MMM
176.70 / 1.69
9.
CH3 of HrHrH
CO of HrHrH
179.73 / 1.18
8.
CH3 MHH + HmHrH
CO of MHH + HmHrH
178.70 / 1.36
7.
CH3 of MmHmM
CO of MmHmM
178.28 / 1.18
6.
CH3 of MrHrM
CO of MrHrM
178.28 / 1.22
5.
CH3 of MrHmM
CO of MrHmM
178.25 / 1.36
4.
CH3 of MrMrH
CO of MMH
177.30 / 1.20
3.
CH3 of MmMrH
CO of MMH
177.30 / 1.27
2.
CH3 of MmMmH
CO of MMH
      177.30 / 1.35
1.
Coupled to Proton of
Type of Carbon
Peak Position(2D HMBC; 13C/1H; ppm)
S.
No.

---
Composition Determination of HEMA/Styrene Copolymers
Composition Determination of HEMA/Styrene Copolymers
Copolymer composition data of H/S
copolymers
The 1H NMR spectrum of H/S copolymer (FH = 0.47)
0.75
0.80
HS7
7.
0.67
0.70
HS6
6.
0.61
0.60
HS5
5.
0.56
0.50
HS4
4.
0.47
0.40
HS3
3.
0.28
0.20
HS2
2.
0.20
0.10
HS1
1.
FH
fH
Copolymer symbol
S.
No.
FH =

---
Reactivity Ratios Determination
Reactivity Ratios Determination
Kelen Tudos (KT) method
rH = 0.64 ± 0.22
rS = 0.41 ± 0.09
Error in Variables method (EVM)
rH = 0.62
rS = 0.40

---
13C {1H} NMR Studies
The DEPT-135 NMR spectrum of H/S copolymer. (FH = 0.47)
The 13C1H} NMR spectrum of H/S copolymer
(FH = 0.47)

---
-CH3 carbon resonances of H/S copolymers from 13C{1H} NMR
-CH3 carbon resonances of H/S copolymers from 13C{1H} NMR
Assignment of -CH3 carbon resonances of
H/S copolymers from 13C{1H} NMR spectra
H/S copolymers with compositions (FH =)a)1.00: b) 0.75,
c) 0.67, d) 0.47 and e) 0.20 in DMSO-d6 at 80°C.
21.20
SrHmS
6.
20.75
SrHrS
5.
19.80
HrHmS
4.
18.20
HrHmH
3.
17.50
HrHrS
2.
16.25
HrHrH
1.
Peak Position
(13C{1H}NMR; ppm)
Peak Assignments
Peak No.

---
The expanded carbonyl carbon regions of H/S copolymers with compositions (FH = a)1.00, b) 0.75, c) 0.67, d) 0.47 and e) 0.20 .
Assignment of carbonyl carbon
resonances of H/S copolymers
SrHmS
175.15
6.
HrHmS
175.45
5.
SrHrS + HmHmH
175.75
4.
HrHmH
176.40
3.
HrHrS
176.60
2.
HrHrH
177.40
1.
Assignment
Peak Position
(13C{1H}NMR; ppm)
S.
No.

---
Assignment of various carbon resonance of H/S copolymers from 2D HSQC spectra
Assignment of various carbon resonance of H/S copolymers from 2D HSQC spectra
The expanded 2D HSQC spectra of H/S copolymers with composition (FH =): a) 0.20, b) 0.47 and c) 0.75 in DMSO-d6
66.0 / 3.85
HH (-OCH2)
12.
66.0 / 3.40
SH / HS (-OCH2)
11.
66.0 / 3.05
SS (-OCH2)
10.
-OCH2 region
58.20 / 3.48
HH (-CH2O)
9.
58.20 / 3.30
SH / HS (-CH2O)
8.
58.20 / 3.05
SS (-CH2O)
7.
-CH2O region
38.50 / 2.45
HSH
6.
38.57 / 2.30
SSH
5.
39.50 / 1.80
SSS
4.
Methine region
45.50 /1.45
SS
3.
47.60 / 1.60
HS
2.
51.50 /1.75
HH
1.
β-methylene region
2D HSQC 13C{1H} (ppm)
Assignment
S.No.

---
The 2D TOCSY spectrum of -methylene carbon region of H/S copolymers with composition (FH =): a) 0.20, b) 0.47 and c) 0.75 in DMSO-d6
The 2D TOCSY spectrum of -methylene carbon region of H/S copolymers with composition (FH =): a) 0.20, b) 0.47 and c) 0.75 in DMSO-d6

---
The 2D TOCSY spectrum of –CH2O and –OCH2 regions of H/S copolymers with composition (FH =): a) 0.47 and b) 0.75 in DMSO-d6 at 80°C.
The 2D TOCSY spectrum of –CH2O and –OCH2 regions of H/S copolymers with composition (FH =): a) 0.47 and b) 0.75 in DMSO-d6 at 80°C.

---
1H-1H cross correlation between non-equivalent geminal protons in H/S copolymers observed from 2D TOCSY spectra.
1H-1H cross correlation between non-equivalent geminal protons in H/S copolymers observed from 2D TOCSY spectra.
4.82 / 3.55
-CH2O (Ha)
-OH
7'
4.56 / 3.28
-CH2O (Hb)
-OH
6'
3.90 / 3.56
-CH2O (Hb)
-CH2O (Ha)
5'
2.50 / 1.90
-CH2 of HH
-CH in HSH
4'
2.35 / 1.85
-CH2 of HH
-CH in SSH
3'
2.32 / 1.55
-CH2 of HS
-CH in SSH
2'
1.85 / 1.30
1.85 / 1.30
-CH2 of SS
-CH2 of SS
-CH of (SSS),
-CH2 of HH
1'
Proton II
Proton I
Peak Position
[TOCSY, 1H/1H, ppm]
Coupled Protons
Correlation peak No.

---
New Observations
New Observations
The reactivity ratio of co-monomers in 2-HEMA – styrene (H/S) copolymers are rH = 0.62 and rS = 0.40 while for 2-HEMA – methyl methacrylate copolymers are rH = 3.32 and rM = 0.23
The complex and overlapped 1H and 13C {1H} NMR spectra of the copolymers were resolved with the help of DEPT -135 and 2 D –HSQC spectra.
The carbonyl carbon of H- unit was assigned upto triad compositional and configurationally sequences in 13C {1H} NMR spectrum.
The methyl carbon signals were assigned upto triad compositional and configurational sequences, whereas β methylene carbon resonances were assigned upto diad compositional sequences.
The methine carbon of M- unit was assigned upto triad compositional sequences.
The various proton and carbon resonance signals of Poly (HEMA) were found to be sensitive to different tacticity sequences

---
Achievements
The micro structure of 2-HEMA copolymers have been studied in detail through NMR spectroscopy. 2- HEMA copolymers with methyl methacrylate and with styrene were found to be sensitive towards compositional and configurationally sequences. Poly 2- HEMA was also found to be tacticity sensitive.
2-HEMA copolymers are biomedically very important due to their properties e.g. Tg, thermal stability and mechanical properties that are dependent on the microstructure of copolymers. It is essential to characterize the microstructure of copolymers which is backbone of all molecular properties. It is important to correlate various properties of copolymers with molecular variations. On this basis, copolymers of desired properties i.e. model compounds can be synthesized.

---
 Research work which remains to be done under the project
In third year, Copolymers of 2-HEMA with 2-Vinyl pyridine, methacrylonitrile and with N-Vinyl pyrrolidone were prepared by free radical bulk polymerization, their microstructure will be determined using NMR spectra.
.

---
List of Publications from this Project
Microstructure determination of 2 - Hydroxy Ethyl Methacrylate - Methyl acrylate Copolymers By NMR Spectroscopy. Sunita Hooda, A.S. Brar and A.K. Goyal, J. Mol. Str. 828 (2007) 25-37.
Structure investigation of 2-Hydroxy Ethyl Methacrylate - Styrene Copolymers by NMR spectroscopy. Sunita Hooda, A.S. Brar and A.K. Goyal, Ind. J. Chem., 45 (A), 1981, 2006.
Stereo chemical configuration of Poly ( 2- Hydroxy ethyl methacrylate ) by NMR spectroscopy. Sunita Hooda, Ind. J. Chem. Accepted, Jan.2007.
NMR studies of 2-Hydroxy Ethyl Methacrylate – methyl methacrylate Copolymers. Sunita Hooda, Under Preparation, 2007.
Papers Presented in Conferences
“Structure Investigation of 2 - HEMA - Methyl acrylate Copolymers By 1D and 2D NMR Spectroscopy.” Sunita Hooda, A.S. Brar and A.K. Goyal, Sent in conference on ”NMR of Polymers", in Gulmarg,held in Oct.2005.
“Synthesis and Design of New Tailor Made Materials for Ions Selective Electrode”. Sunita Hooda and Vandana Uberoi; Presented in 9th CRSI National Symposium in Chemistry, Organized by the Dept of Chemistry, University of Delhi, Feb 1-4 2007.